The Graduate MSE Program at Washington State University

&

Challenges in 3-D integration in Microelectronics: Using Materials Science to Predict Complications and Provide Solutions

Indranath Dutta

Materials Science and Engineering Program and

School of Mechanical and Materials Engineering

Washington State University

Pullman, WA 99164

ABSTRACT

This talk will start with an overview of the interdisciplinary Materials Science and Engineering Program (MSEP) at WSU.  This will be followed by a technical presentation on Materials research in the speaker's group.

The technical talk will present two aspects of near-interface multi-physics interactions in materials, as applicable to the reliability of electronic devices and packages.

First, the phenomenon of electromigration-assisted interfacial sliding, where combined thermal, mechanical and electrical fields cause relative motion between two adherent components (e.g., a metal and a semiconductor), will be introduced.  Examples and mechanisms of this in both solid-solid and solid-liquid interfaces will be presented.  Potential implications of this phenomenon for the reliability of through-silicon via (TSV) structures in 3-D devices will be discussed.

Secondly, the role of process and service conditions on lead-free solder microstructures, and consequently on fracture properties of solders, will be presented.  Methodologies for developing fracture mechanism maps will be elucidated.  The implications for solder joint reliability under drop conditions, particularly in 3-D packages, will be discussed.

________________________________________________________________________

Indranath Dutta is Professor of Mechanical and Materials Engineering and Director of the Materials Science and Engineering Program at Washington State University (WSU), where he also served as Associate Dean of the College of Engineering and Architecture during 2011-2013. He received a B. Tech. from the Indian Institute of Technology (Kharagpur) in 1983, a M.S. from Case Western Reserve University in 1985, and a PhD from the University of Texas at Austin in 1988.  Prior to joining WSU, he was Professor of Materials Science and Mechanical Engineering at the Naval Postgraduate School (1988-2008).  He has held visiting positions at the Air Force Research Laboratory (1995), the University of Oxford (1996), MOTOROLA (2000), INTEL Corporation (2001), and Nanyang Technological University, Singapore (2008). He is a Fellow of ASM International.

Prof. Dutta's current research is in the area of multi-physics phenomena in multi-component materials systems, with emphasis on materials for microelectronics and meso-to-nanoscale electrically-activated manufacturing processes.