The Silver-Indium Binary System and Its Electronic Packaging Applications

Chin C. Lee

Electrical Engineering and Computer Science

Materials and Manufacturing Technology

University of California, Irvine, CA 92697-2660

cclee@uci.edu  tel: 949-824-7462  fax: 949-824-3732

Abstract

The silver-indium (Ag-In) binary system is reviewed. This system has never been used in electronic industries except In-Ag eutectic for bonding laser diode chips. It was chosen for our packaging process development because of its forward looking possibilities that other systems do not possess. Conventional die-attach materials and fluxing action in soldering processes are briefly presented. Several processes dealing with tin oxides are mentioned. Our fluxless bonding is then introduced. Four fluxless bonding designs using the Ag-In system are reported. All joints produced have melting temperature higher than 700°C. Samples of the third design survived 5,000 thermal cycles between -40 to +200°C. The fourth design survived storage at 350°C for 200 hours.

To understand the mechanical properties of Ag, the solid solution phase (Ag), and intermetallic compound Ag3In, ingots have been grown. ASTM tensile test (TT) samples are prepared. (Ag)-20In TT samples exhibit superior tensile properties compared to pure Ag. Reaction experiments with sulfur (S) vapor shows that the reaction rate with (Ag)-20In is much lower than that with pure Ag. It seems that (Ag)-20In has the anti-tarnishing properties that the metallurgical community has been looking for several centuries. More quantitative reaction experiments on (Ag) are being conducted.

Ag has superior physical properties. The challenge and limit in its electronic and optical applications are tarnishing. It reacts easily S and H2S to form Ag2S which is black and fragile. It also reacts easily with chlorine (Cl) to form AgCl. Our preliminary results on the properties of (Ag)-20In seem to indicate that (Ag) solid solution might be an answer.

Biography

Chin C. Lee was born in Taiwan. He received B.E. and M.S. degrees in electronics from National Chiai-Tung University, Taiwan, and Ph.D. degree in electrical engineering from Carnegie-Mellon University.

He is a professor of electrical engineering and computer science at the University of California, Irvine, where he also serves as the Director of school-wide Materials and Manufacturing Technology graduate program. His research activities include acoustic waves, bonding technology, electromagnetic theory, electronic packaging, metallurgy, microwave devices, optoelectronics, semiconductor devices, and thermal analysis and design. He has co-authored 4 book chapters and more than 250 research papers.

Chin C. Lee is a Life Fellow of IEEE (Institute of Electric and Electronic Engineers, Inc.), a Fellow of Photonics Society of Chinese-Americans, and a member of Tau Beta Pi. He has served as an associate editor of IEEE Trans. on Components, Packaging and Manufacturing Technology (CPMT) for 21 years. Since 1998, he has been on the Program Committee of IEEE Electronic Components and Technology Conference (ECTC) and served as the Chair of Materials and Processing sub-committee for 4 yours. He also served as the Chair of CPMT Society Technical Committee on Material and Processes in 2013 and 2014.

He received the Best Paper Award for "Diagnosis of hybrid microelectronics using transmission acoustic microscopy" in 1979 IEEE Reliability Physics Symposium, the 2007 IEEE-CPMT Exceptional Technical Achievement Award, and the 2012 IEEE-CMPT Electronic Manufacturing Technology Award. He is listed among highly cited researchers in engineering category on Thomson-ISI Citation Dada Base.